O

TECHNICAL INF

| GARANTİ |  |  |  | 10 years* |  | Environme | nt, health and safety |
| --- | --- | --- | --- | --- | --- | --- | --- |
| YAPI |  |  |  | 83% vinyl - 7% fiberglass - 10% PET |  | Recycled Content | 10% |
| TABAN |  |  |  | Vinyl + Felt |  | Reach | Compliant |
| TOPLAM KALINLIK |  | ISO 1765 |  | 5mm - 0.20" |  | LEED v4 | Compliant (LEED Contributing Product) |
| TOPLAM AĞIRLIK |  | ISO 8543 |  | 3000 g/m² - 88.5 oz/yd² |  | CDPH Standard Method V1.2 | Pass |
| RULO ENİ |  | EN ISO 24341 |  | ca. 200cm - ca. 6'7" |  | BREEAM® International | Compliant |
| RULO UZUNLUĞU |  | EN ISO 24341 |  | ca. 30m - 32.8 yd |  | BREEAM® NOR | Pass |
| KARO BOYUTU Her kutuda 16 adet |  | EN 994 |  | 50cm x 50cm - 19.69" x 19.69" |  | French VOC Regulation | A+ Certified |
| KULLANIM DAYANIKLILIĞI |  | EN 1307 ASTM D5252 |  | Class 33 Heavy commercial use |  | French CMR components | Pass |
| YÜRÜME TRAFİĞİ TESTİ |  | ASTM D6119-12 |  | Heavy traffic |  | AGBB/ABG | Pass |
| TEKERLEKLİ SANDALYE TESTİ |  | EN 985 |  | Continuous use |  | Belgian VOC Regulation | Pass |
| YANGINA DAYANIKLILIK |  | EN 13501-1 |  | Bfl-s1 |  | Indoor Air Comfort Gold | Pass |
|  |  | ASTM E 84 UL 723 |  | Class I or A rating |  |  |  |
|  |  |  |  |  |  | Blue Angel (RAL UZ120) | Pass |
| KRİTİK RADYAN AKIŞI |  | ASTM E648-15e1 NFPA |  | 0,84 W/cm² Class I |  | EN 717-1 | E1 |
| DUMAN YOĞUNLUĞU |  | ASTM E622 |  | < 300 |  | M1 Protocol of July 2017 | Pass |
| YÜRÜME TESTİ |  | ISO 6356 AATCC 134-2006 |  | < 2 kv Permanently antistatic |  | Plasticizer Content | Phthalate Free |
| SOLMAZLIK |  | ISO 105-B02 |  | 7 |  |  |  |
| KAYMAZLIK |  | EN 13893 ASTM C1028-07 DIN 51130 EM 13036-4 |  | 0,3 0,85 R9 65 |  |  |  |
| DARBE SESİ AZALTMA |  | ISO 10140 |  | 19dB |  |  |  |
| AKUSTİK EMİLİM |  | ISO 354 |  | w = 0,15 |  |  |  |
| AYAK SESİ AZALTMA |  | EPLF 021029-3 |  | SL70 |  |  |  |
| BOYUTSAL DURAĞANLIK |  | EN 986 ISO 2551 |  | Meets the requirements |  |  |  |
| ISI DAYANIMI |  | ISO 8302 |  | Suitable for underfloor heating |  |  |  |
| CE Certificate |  | EN 14041 |  | 0493-CPR-0151 |  |  |  |
| Co2 neutral on demand * Terms and conditions are available on request |  |  |  |  |  |  |  |

2tec2 • 284 Chaussée d’Aelbeke, 7700 Mouscron, Belgium	info@2tec2.com • www.2tec2.com